## Slide 1
Effect of electronic reservoir on phase transitions in strongly correlated systems
Soumen Bag
Laboratoire de Physique des Solides (LPS), Université Paris-Saclay, France
25 th Jan, GDR Meeting, Collège de France

## Slide 2
Alberto Camjayi
University of Buenos Aires
Marcello Civelli
LPS, Université Paris-Saclay
Marcelo Rozenberg
LPS, Université Paris-Saclay
Lorenzo Fratino
Laboratoire de Physique Théorique et Modélisation
Henry Navarro
University of California, San Diego
Ivan K. Schuller
University of California, San Diego
Theory
Experiment

## Slide 3
Introduction: tuning transition temperature
Insulator to Metal tansition V2O3
Resistance changes 6 order of magnitude.
Resistance switching phonomenon make it interesting for various application like memory storage, nuromorphic computing etc. but the problem is it has transition temperature ~150 K which is well below the room temperature. Where as its cousin VO2 has transition temperature 310 near room temperature.
It is interesting to tune the transition temperature.
Namely pressure, doping, light. Especially, the effect of light on these films is small
V2O3
Large resistance change across the transition can be exploited in neuromorphic device
VO2
Pressure and chemical doping can tune transition.
Easy way to tune the transition temperature?

## Slide 4
Can we control TIMT using light?
CdS/V2O3
CdS/VO2
H. Navarro Appl. Phys. Lett. 118, 141901 (2021)
Can we understand the suppression of TIMT?
Transition temperature decreases with increasing illumination intensity (P) for CdS/V2O3
In principle one can switch from insulating state to metallic state by light.
Transition temperature suppress with increasing illumination intensity (P) for CdS/VO2. But, Suppression is relatively small.

## Slide 5
Minimal Model
HM: J. Trastoy, M. Rozenberg, et. al. PRB, 101:245109 (2020)
DHM: O. Nájera, M. Rozenberg, et. al. PRB, 95(3):035113, 2017
V2O3
Hubbard Model (HM)
VO2
Dimer Hubbard Model (DHM)
arxiv.org/pdf/cond-mat/0210558.pdf
2
Bond(B)
Anti-Bond(AB)

## Slide 6
Minimal model for heterostructure model and method
CdS/VO2
Dimer Hubbard Model (DHM)
How Γ effect the system?
HM: J. Trastoy PRB, 101:245109 (2020)
DHM: O. Nájera PRB, 95(3):035113, 2017
CdS/V2O3
Hubbard Model (HM)
CdS
Parameter of interest is:
We will use DMFT with HYB-CTQMC impurity solver

## Slide 7
We solve impurity model using Hybridization expansion Continuous Time Quantum Monte Carlo (HYB-CTQMC) as impurity solver.
DMFT for Electronic reserver coupled HM
, Where Γ = γ2/D
Where
Integrating out the ‘a’ fermion lead to an effective addition hybridization to the ‘c’ fermions:
DMFT
A. Georges, M.R. et.al. DMFT RMP, 1996
P. werner et.al. HYB-CTQMC, PRL, 2006

## Slide 8
We solve impurity model using Hybridization expansion Continuous Time Quantum Monte Carlo (HYB-CTQMC) as impurity solver.
DMFT for Electronic reserver coupled DHM
Where
DMFT

## Slide 9
Suppression of AFM in HM
PM(M): Paramagnetic (Metal), PM(I): Paramagnetic (Insulator), AFM(I): Antiferromagnet (insulator
At small U, TN ~ exp(∆(U)) at large U is TN ~ t2/U
Heisenberg
Slater
TN decreases with Γ.
Why TN suppress?
ms at low temp decreases
TN

## Slide 10
Suppression of AFM in HM
U=4.0
U=1.7
Kondo effect give rise two peak around zero frequency and responsible to AFM suppression!
Jk

## Slide 11
Experiment and theory for suppression of TIMT in CdS/V2O3
CdS/V2O3
Experiment
Γ
Theory
suppression of Transition temperature TIMT observed in CdS/V2O3
For HM-AFM coupled with metallic bath, Transition temperature suppresses with increasing Γ.
U=1.7

## Slide 12
What happen to the transition as a function of Γ?
IMT in DHM
O. Nájera, M. Rozenberg, et. al.PRB, 95(3):035113, (2017)
L. Fratino, S. Bag, M. Rozenberg, et. al., PRB 105,125140 (2022)
metal
Insulator

## Slide 13
Effect of Γ on the the Mott phase of DHM
Bond(B)
Anti-Bond(AB)
AB and B form kondo singlet with reservoir’s electron
U=2.2
U=4.0

## Slide 14
Experiment and theory for suppression of TIMT in CdS/VO2
Experiment
Theory
Γ
suppression of Transition temperature TIMT observed in CdS/VO2
For DHM coupled with electronic reervoir, Transition temperature suppresses with increasing Γ.

## Slide 15
conclusion
Hubbard model coupled with a electronic reservoir could capture the suppression of IMT observed in CdS/V2O3 by light.
Dimer Hubbard model coupled with electronic reservoir capture the suppression of IMT observed in CdS/VO2 by light. But it overestimate the transition
The coupling to the lattice structure of the electronic degrees of freedom of VO2,which is absent in our simplified model
Thanks for your attention!