## Slide 1: Eutectics of (Al2O3-YAG):Ce for Phosphor Converters of White Solid-State Lighting Driven by Laser Diodes
Oleh Vovk
ICMCB, Bordeaux
Institute for Single Crystals, Kharkiv

## Slide 2: Motivation. Development of LD WSSL

## Slide 3: Selected Rules for Laser Phosphors
Small luminescence saturation
Small thermal saturation
High quantum efficiency
Small Stokes shift
Low thermal quenching
High thermal conductivity
Effective heat dissipation
Small optical saturation
Short decay time
Uniform light distribution and high extraction efficiency
Suitable light scattering
Thermal and radiative resistance of the phosphors.
High chemical stability, non reacting with environment (О2, СO, CO2, H2O).
S. Li, L. Wang, N. Hirosaki, R., Laser Photonics Rev. 2018

## Slide 4: Selected Rules for Laser Phosphors
Small luminescence saturation
Small thermal saturation
High quantum efficiency
Small Stokes shift
Low thermal quenching
High thermal conductivity
Effective heat dissipation
Small optical saturation
Short decay time
Uniform light distribution and high extraction efficiency
Suitable light scattering
Thermal and radiative resistance of the phosphors.
High chemical stability, non reacting with environment (О2, СO, CO2, H2O).
S. Li, L. Wang, N. Hirosaki, R., Laser Photonics Rev. 2018
YAG:Ce
YAG:Ce
YAG:Ce + Al2O3
YAG:Ce + Al2O3

## Slide 5: Light-harvesting model in light converter with dispersion medium of internal diffusers
Schematic diagram of binary crystalline system for realizing incandescent, high-power white-light-emitting diodes along with comparative information regarding conventional particle-dispersed system.
The exhibition of the blue light being absorbed and converted by Ce3+ (a) and the light propagation (b) in single Ce:YAG matrix and in Ce:YAG matrix with Al2O3 particles, the critical angle φc = 33°. Y. Tang et al Optics Express, 2015
Ishikawa et al, Int. J. Appl. Cer. Techn. 2006.
Estimation according our model results in rising light yield output from 8 to 16 % for the scattering media

## Slide 6: Eutectics Al2O3-YAG:Ce. Experimental scheme and sample morphology
Morphology of the different ingots of the Al2O3-YAG:Ce eutectics
z
x
y
Crystal axis
Scheme of the horizontal directed crystallization (HDC) setup
Typical ingot of eutectic Al2O3/YAG:Ce, 1 at% Ce
Notes: We have synthesized and investigated the alumina yttrium aluminum garnet eutectics doped with CE as phosphor for laser lighting
Al2O3 –YAG:Ce eutectic has been synthesized by the HDC technique. The composition of eutectics was taken according well know phase diagram with correction on the Ce amount.
Description of the HDC
Desciption of the experiment
Desciption of the morphology: two phases, mutual penetration, cellular growth
Phases are corundum and YAG that proven by XRD
Typical crystal
Dependence of morphology from grown conditions rate of crystallization

## Slide 7: Morphology of Al2O3/YAG:Ce eutectics
SEM Al2O3/YAG:Ce, 0 at% Ce, 50 mm/h
SEM Al2O3/YAG:Ce, 0.25 at% Ce,15 mm/h
Dependance евт on V: 1) theoretical, евт2V=const, 2) experimantal, евт1,75V=const
Dependance max. length of chord on С(Се)

## Slide 8: Structural perfection of the crystal boundaries. TEM and HRTEM

## Slide 9: Structural perfection of the YAG crystal in eutectics. HRTEM and EDS

## Slide 10: Garnet crystal structure of Y3Al5O12
Schematic diagram of the electronic levels of Ce3+ in YAG
Local structure of a dodecahedral position and schematic dodecahedral framework

## Slide 11: Luminescent properties, PL and PLE spectra
PL emission spectra (a) and PLE spectra (b) of (Al2O3-YAG):Ce eutectic (sample 4) under excitation at different wavelengths (a) and registration of Ce3+ luminescence in the garnet ((b), curve 1) and sapphire phase ((b), curve 2). A.Shahno Materials 2023, 16, 2701 https://doi.org/10.3390/ma16072701

## Slide 12: Decay kinetics of (Al2O3-YAG):Ce eutectic
Decay kinetics of (Al2O3-YAG):Ce eutectic corresponding to the Ce3+ luminescence in the YAG:Ce (1) and Al2O3:Ce (2) phases under excitation in the respective PLE bands at 450 nm (1) and 270 nm (2). A.Shahno Materials 2023, 16, 2701 https://doi.org/10.3390/ma16072701

## Slide 13: Thermal properties of the Al2O3-YAG:Ce eutectics. Laser Flash Analysis
Thermal diffusivity of the Al2O3-YAG:Ce eutectic composite
Principles of the LFA
·
λ(T)= a(T) · ρ(T) · cp(T)
a: Thermal diffusivity ρ: Density, cp: Specific heat capacity, λ: Thermal conductivity, T: Temperature
Thermal conductivity eutectic composite

## Slide 14: Kinetics of sample temperature under laser irradiation
2D heat distribution in sample # 1 a) and sample # 4 b) under blue diode laser excitation with optical power P=937 mW at different time intervals (after 10s, 25s, 36s, 46s, 85s and 360s) (compare Fig. 3).

## Slide 15: Dependence of the thermal behavior of Al2O3-YAG:Ce eutectics on morphology
Sample photos
SEM images
Thermal images
Kinetics of the horizontal temperature distribution

## Slide 16: Radiometry under laser excitation at 450 nm
sample | Efficiency, Lm/W | Efficiency, % | Sensitivity, Lm/W
# 2 | 231 | 62 | 370
# 3 | 267 | 68 | 394
# 4 | 234 | 63 | 373
# 5 | 172 | 50 | 342
СІЕ diagram of Al2O3/YAG:Ce eutectics, without LD
СІЕ diagram of Al2O3/YAG:Ce eutectics

## Slide 17: Conclusion
Al2O3-YAG:Ce eutectics meets the requirements to phosphor converter for high power White Solid State Lighting driven by Laser Diodes

## Slide 18: Our colleagues who collaborate in the work
Institute of Physics NAS Ukraine, Kyiv
Institute Low Temperature and Structural Research, Polish Academy of Sciences, Wroclaw
Institute of Physics, PAS, Warsaw
Institute of Electronic Materials Technology, Warsaw
Kazimierz Wielki University in Bydgoszcz, Bydgoszcz
Universidad Autónoma de Madrid, Madrid

## Slide 19: Thank for attention