## Slide 1: Ultrafast Structural Dynamics and Control of Phase Transitions
Herve Cailleau
Institute of Physics of Rennes
International Research Laboratory DYNACOM Tokyo
M. Lorenc, E. Janod, C. Mariette, S. Iwai, …

## Slide 2
From pioneering works
Neutral-Ionic PIPT Coherent phonon
S. Koshihara K. Sokolowski-Tinten
PRB 1990 Nature 2003

## Slide 3
Relaxations of Excited States
and Photo-Induced Phase Transitions

## Slide 4
Ultrafast Techniques
as fast as atomic motions
Pump-probe method
Optical (IR-UV)
Thz and mid-IR
X-ray and
electron diffraction
XANES
- ARPES
…
Currently 10-100 fs
Nphot ~ few percent
E ~ 1-100 MV/cm (10-2-1 V/Ǻ)

## Slide 5
Ultra-fast X-ray science
around large facilities:
synchrotron 100 ps
X-FEL 10-100 fs

## Slide 6
Ultra-fast X-ray science
around large facilities:
synchrotron 100 ps
X-FEL 10-100 fs
coupled to very sentive transient
optical reflectivity measurents

## Slide 7
To « towards properties on demand in quantum materials »
Review
Basov, Averitt,
Hsieh
Nature Materials
September 2017
« New eyes give rise
to new ideas »
Not only seeing
but also acting
Thermal PT/PIPT

## Slide 8
Outline
1 – Isosymetric and/or Symmetry Breaking Phase Transitions
2 – Ultrafast Structural Dynamics and Control of Phase transitions

## Slide 9
Outline
1 – Isosymetric and/or Symmetry Breaking Phase Transitions
2 – Ultrafast Structural Dynamics and Control of Phase transitions

## Slide 10
Phase transitions: a long story since Van der Waals
More one century was necessary to establish the universality of phase transitions at thermal equilibrium, despite the diversity in the nature of constituents, interactions and properties
.

## Slide 11
Phase transitions: a long story since Van der Waals
More one century was necessary to establish the universality of phase transitions at thermal equilibrium, despite the diversity in the nature of constituents, interactions and properties
The familiar example is the liquid-gas phase transition
with T and P as external control parameter.
Phase diagram exhibits a first order phase transition
located on a coexistence line P0(T) ending at a
critical point C, below the supercritical crossover
regime.
No change of symmetry
A thermodynamic rule:
T increase favours the phase of high-entropy S
P increase favours the phase of low-volume V
dP/dT = ΔS/ΔV
.

## Slide 12
Phase transitions: a long story since Van der Waals
A quantum material
Metal – Insulator Mott
transition
Lang et al.
Science Advances 2016
Κ-(BEDT-TTF)2Cu[N(CN)2]Cl

## Slide 13
Phase transitions: a long story since Van der Waals

## Slide 14
Phase transitions: a long story since Van der Waals
Not unique
A quantum material
Cerium
Decremps et al.
PRL 2011
Analogy with Van der Waals
equation of state
Very large change of volume

## Slide 15
Universality with the phase transition of a ferromagnetic material
For the para-ferromagnetic phase transition in a magnetic fluid the control parameters are T and H.
The situation is very similar but now in the phase diagram the coexistence line
is now located on the horizontal axis H = 0.

H
Tc T
C
M>0
M<0

## Slide 16
Universality with the phase transition of a ferromagnetic material
For the para-ferromagnetic phase transition in a magnetic fluid the control parameters are T and H.
The situation is very similar but now in the phase diagram the coexistence line
is now located on the horizontal axis H = 0.

H
Tc T
C
M>0
M<0
What we call boils down to follow the horizontal
axis at H = 0 and it is associated with the
establishement of a spontaneous magnetic order
below TC.
Kinetics after thermal quench: formation of
domains

## Slide 17
Universality with the phase transition of a ferromagnetic material
For the para-ferromagnetic phase transition in a magnetic fluid the control parameters are T and H.
The situation is very similar but now in the phase diagram the coexistence line
is now located on the horizontal axis H = 0.

H
Tc T
C
M>0
M<0
Crossing the 1st order transition line at H = 0
discontinuity of M for T < Tc (magnetic hysteresis),
but not of S : ΔM ≠ 0 and ΔS = 0 → dH/dT = 0
Kinetics : nucleation-growth from one phase M < 0
to another one M > 0

## Slide 18
Universality with the phase transition of a ferromagnetic material
For the para-ferromagnetic phase transition in a magnetic fluid the control parameters are T and H.
The situation is very similar but now in the phase diagram the coexistence line
is now located on the horizontal axis H = 0.

H
Tc T
C
M>0
M<0
Crossing the 1st order transition line at H = 0
discontinuity of M for T < Tc (magnetic hysteresis),
but not of S : ΔM ≠ 0 and ΔS = 0 → dH/dT = 0
Kinetics : nucleation-growth from one phase M < 0
to another one M > 0

## Slide 19
Universality with the phase transition of a ferromagnetic material
For the para-ferromagnetic phase transition in a magnetic fluid the control parameters are T and H.
The situation is very similar but now in the phase diagram the coexistence line
is now located on the horizontal axis H = 0.

H
Tc T
C
M>0
M<0
Crossing the 1st order transition line at H = 0
discontinuity of M for T < Tc (magnetic hysteresis),
but not of S : ΔM ≠ 0 and ΔS = 0 → dH/dT = 0
Kinetics : nucleation-growth from one phase M < 0
to another one M > 0

## Slide 20
Stability, metastability
and instability
Symmetry breaking / Isosymmetric phase transition
F
M
Symmetry breaking
para-ferromagnetic
Isosymmetric
gas-liquid
H
Landau free energy landscape F = Aη2 + Bη4 - Hη

## Slide 21
Stability, metastability
and instability
Symmetry breaking / Isosymmetric phase transition
F
M
Symmetry breaking
para-ferromagnetic
Isosymmetric
gas-liquid
H
Landau free energy landscape F = Aη2 + Bη4 - Hη

## Slide 22
Stability, metastability
and instability
Symmetry breaking / Isosymmetric phase transition
F
M
Symmetry breaking
para-ferromagnetic
Isosymmetric
gas-liquid
H
Landau free energy landscape F = Aη2 + Bη4 - Hη

## Slide 23
Landau theory
Every dens,ity is expressed as (r) = 0(r) + (r), where 0 is left invariant by all elements of the HS group G0 and  by only the elements of an irreductible representation (IR) of the initial group G0, i.e. a group-subgroup relation G  G0. The lost of symmetry elements (Symmetry Breaking) is desribed by an order parameter  of dimension equal to that of the IR.
Landau symmetry breaking analysis

## Slide 24
Landau theory
Every dens,ity is expressed as (r) = 0(r) + (r), where 0 is left invariant by all elements of the HS group G0 and  by only the elements of an irreductible representation (IR) of the initial group G0, i.e. a group-subgroup relation G  G0. The lost of symmetry elements (Symmetry Breaking) is desribed by an order parameter  of dimension equal to that of the IR.
At thermal equilibrium, different kind of degrees of freedom (electronic, structural, …) follow the evolution of this quantity measuring the degree of SB.
But in case of PIPT decoupling in time occurs?
Another fundamental feature is the formation of non-homogeneneous textured LS state, the domain structure, associated with the different equivalent phases.
What influence on PIPT?
Landau symmetry breaking analysis

## Slide 25
Stability, metastability
and instability
Symmetry breaking + Isosymmetric phase transitions
Symmetry breaking order parameter + Totally Symmetric order parameter

## Slide 26
Stability, metastability
and instability
Symmetry breaking + Isosymmetric phase transitions
Ferroelecric symmetry breaking + Totally symmetric ionicity
N- I transition in TTF-CA
PRL 1997
From N band insulator
to I Mott insulator
Lemée-Cailleau
PRL 1997

## Slide 27
Stability, metastability
and instability
Symmetry breaking + Isosymmetric phase transitions
Ferroelecric symmetry breaking + Totally symmetric ionicity
N- I transition in TTF-CA
Lemée-Cailleau
PRL 1997

## Slide 28
Symmetry breaking + Isosymmetric phase transitions
V2O3 prototypical Mott material
Ferroelastic symmetry breaking + Totally Symmetric I-M

## Slide 29
Symmetry breaking + Isosymmetric phase transitions
V2O3 prototypical Mott material
Ferroelastic symmetry breaking + Totally Symmetric I-M

## Slide 30
Symmetry breaking + Isosymmetric phase transitions
V2O3 prototypical Mott material
Ferroelastic symmetry breaking + Totally Symmetric I-M
From Kanoda PRB 2018

## Slide 31
Beyond the Hubbard model, taking into account only electronic degrees of freedom, the coupling to lattice degrees of freedom and the long range nature of elastic interactions changes the nature of the phase transitions:
all Mott transitions couple to elastic degrees of freedom,
many possible structural symmetry breakings,
- phonon entropy dominates to stabilize the metallic phase,
from P. Littlewood ECRYS 2022
Role of structural degrees of freedom

## Slide 32
Beyond the Hubbard model, taking into account only electronic degrees of freedom, the coupling to lattice degrees of freedom and the long range nature of elastic interactions changes the nature of the phase transitions:
all Mott transitions couple to elastic degrees of freedom,
many possible structural symmetry breaking,
- phonon entropy dominates to stabilize the metallic phase,
from P. Littlewood ECRYS 2022
« The only interaction known which is truly infinitely long range »
J. Friedel 1954
Role of structural degrees of freedom

## Slide 33
Beyond the Hubbard model, taking into account only electronic degrees of freedom, the coupling to lattice degrees of freedom and the long range nature of elastic interactions changes the nature of the phase transitions:
all Mott transitions couple to elastic degrees of freedom,
many possible structural symmetry breaking,
- phonon entropy dominates to stabilize the metallic phase,
from P. Littlewood ECRYS 2022
« The only interaction known which is truly infinitely long range »
J. Friedel 1954
What about ultrafast photoinduced phase transitions?
Role of structural degrees of freedom

## Slide 34
Outline
1 – Isosymetric and/or Symmetry Breaking Phase Transitions
2 – Ultrafast Structural Dynamics and Control of Phase transitions

## Slide 35
Diversity of photoexcitation processes
Delocalized (Peierls)
CT exciton
Localized (molecular switching)

## Slide 36
Multiscale dynamical processes in the solid state
Strain propagation
Electronic motion
1 s
10-3 s
10-6 s
10-15 s
days
Atomic oscillation
Different time
scales
10-9 s
10-12 s
10-15 s
Thermal processes?

## Slide 37
Bottlenecks during the evolution
M. Lorenc
PRL (2009)
PRB (2012)
W W
Q
Spin transition
From molecule to material
scale

## Slide 38
Coherent collective dynamics of atomic motions
time
amplitude

## Slide 39
Coherent oscillating atomic motions
Driven by the quasi-instantaneous
change of the electronic state
induced by photoexcitation.
displacive force Fq=0 ≠ 0
selective vs. democratic
Bragg peak Debye-Waller
oscillation Diffuse scattering

## Slide 40
Coherent oscillating atomic motions
Driven by the quasi-instantaneous
change of the electronic state
induced by photoexcitation.
displacive force Fq=0 ≠ 0
The dynamics of Q0 is governed by
a displaced potential energy
Bilinear coupling ~ ΔnelQ0
Displaced minimum in ES(Q)
From S. Johnson
Son et Lumière
Les Houches
2019
Time scale:
period of
optical
mode

## Slide 41
Optical mode softening
K. Sokolowski 2011
Se = Cst

## Slide 42
Coherent oscillating atomic motions
Driven by the quasi-instantaneous
change of the electronic state
induced by photoexcitation.
Bilinear coupling ~ ΔnelQ0 Linear-quadratic ~ ΔnelQkQ-k
Displaced minimum in ES(Q) Change of curvature
From S. Jonhson
Son et Lumière
Les Houches
2019
Time scale:
period of
optical
mode
Q0(t) <(ΔQk)2>

## Slide 43
B. Arnaud PRL 2013
Debye-Waller and diffuse scattering effect
Bismuth

## Slide 44
B. Arnaud PRL 2013 S. L. Johnson PRL 2009
Debye-Waller and diffuse scattering effect
Bismuth
Squeezed
phonon
oscillation

## Slide 45
Photoinduced strain wave dynamics
Initially, just after photoexcitation the volume has not changed and stress energy
is stored (thermal or non-thermal). To recover mechanical equilibrium with ouside
pressure longitudinal strain wave are launched from interfaces (air/film and
film/substrate). → acoustic phonons counterpart / optical phonons.

## Slide 46
Photoinduced strain wave dynamics
Just after photoexcitation the volume has not changed and elastic stress energy
is stored (thermal or non-thermal). To recover mechanical equilibrium with ouside
pressure longitudinal strain wave are launched from interfaces.
→ acoustic phonons counterpart / optical phonons.
Thin Substrate Thick Substrate
Acoustic time scale
tac = d/vs
For t ≥ 2tac
stabilization in
new equilibrium
volume.
From M.Bargheer
Structural Dynamics
2014

## Slide 47
Cooperativity – Nonlinear Responsiveness - Threshold
S. Iwai PRL (2006)
After ultrafast photoexcitation, a
new potential energy landscape
for the equlibrium states (phases)
in the order parameter space
and the laser fluence is now the
control parameter.

## Slide 48
Cooperativity – Nonlinear Responsiveness - Threshold
SCO Isosymetric transition
R Bertoni et al.
Nature Materials 2016

## Slide 49
Cooperativity – Nonlinear Responsiveness - Threshold
Mott V2O3
I to M transition in
granular thin film
Preprint

## Slide 50
Cooperativity – Nonlinear Responsiveness - Threshold
Mott V2O3
I to M transition
Granular thin film
Preprint
Full I to M transformation

## Slide 51
Bottlenecks: role of morphology on propagative deformations
Bargheeer Photoacoustics 2023

## Slide 52
In the wake of strain waves
Mott V2O3
I to M transition ingranular thin film
Preprint
c.f Poster Julio Guzman
The volume dynamics scales with the film thickness
The shear dynamics scales with the ferroelastic domain size
The electronic dynamics (transient reflectivity)
follows the structural dynamics

## Slide 53
Universality of strain wave pathway
Strong similarities with the N-I transition in TTF-CA
S. Iwai PRB 2004

## Slide 54
Bottlenecks: anisotropy in propagative transition
N-I transition M. Buron-Lecointe
in TTF-CA PRB 2003
~
SCO K. Boukheddaden
PRL 1995
Thermal interface motion (~ μm/s) vs. sound velocity (~ km/s)

## Slide 55
Four main lessons
From kinetics to dynamics
Different isosymmetric/Symmetry breaking dynamics
Crucial role of morphology for efficiency
Central role of volume and elastic cooperativity

## Slide 56
Elastic cooperativity reinforces the electronic one
Electronic cooperativity
On a two orbital model (Fabrizio PRB 2015), the excess population of ele
in upper orbital and holes in lower orbital may lead to a gap collapse above
Athreshold. The more the excess population increases, the more the effective
gap deceases.
+ Elastic cooperativity
Compressive stresses induce positive chemical pressure.When the density of
excited electrons increases, chemical pressure increases proportionality, i.e.
as an intermal mean field inducing positive feedback.

## Slide 57
Precursor processes ?
Small polarons ?

## Slide 58
Small polaronic states
V – O shorter V – V shorter
Energy gain (self-trapping) ≈ 100 meV
D. Wickramaratne PRB 99, 214103 (2019)
Spatial self-trapping → small polaron

## Slide 59
Strain wave pathway
- from local precursors at nanoscale
1-10 molecules
F. Morrissey
PRB
2010
cf. S. Nasu’s
talk

## Slide 60
Strain wave pathway
- from local precursors at nanoscale
- to phase transition at macroscale
1-10 molecules
F. Morrissey
PRB
2010
Generalization to shear strains (ferroelastic)
cf. S. Nasu’s
talk
Phase front propagation at
sound velocity
From kinetics to dynamics
of phase transition

## Slide 61
Bottlenecks: incomplete efficiency in pellet of nanocrystals of Ti3O5

## Slide 62
A.M. Linderberg
Science 2021
Similarities between transient
structural changes formed under
electrical and optical excitation
Towards the AI challenge

## Slide 63
From band insulator to Mott insulator – Electronic ferroelectricity
A band insulator is qualitively different from a Mott insulator, topologically distinct (Berry Phase jumps by π). Across the transition, the static ionic charges are quasi-continuous, while the Born charges changes sign (Resta PRL 1995). In the Mott state the anion transports a positive charge.

## Slide 64
From band insulator to Mott insulator – Electronic ferroelectricity
A band insulator is qualitively different from a Mott insulator, topologically distinct (Berry Phase jumps by π). Across the transition, the static ionic charges are quasi-continuous, while the Born charges changes sign (Resta PRL 1995). In the Mott state the anion transports a positive charge.
In its modeling of N-I transition
Painelli (Crystals 2017)
observes a discontinuous
change of sign for ΔPe.

## Slide 65
Relaxations of Excited States
and Photo-Induced Phase Transitions
Thank you