## Slide 1
Romain GAUTIER
Institut des Matériaux de Nantes Jean Rouxel (IMN)
GDR MEETICC
Nantes, December 5th, 2023
Machine Learning Guided Synthesis of Materials with Specific Structures and Properties
Chemist interested in ML.
L’objecif, ici, n’est pas vraiment de rentrer dans les détails technique du ML mais de voir comment le ML peut être utilisé pour la science des matériaux.

## Slide 2
What is Artificial Intelligence?
Symbolic AI
Connectionist AI
Hypothetical-deductive machine
Inductive machine
First use of the term “Artificial Intelligence”
Machine Learning belongs to this category
Cardon D.; Cointet, J.P..; Mazières, A. “Neurons spike back”, Réseaux, (2018) 211(5)
Notes: 2
2

## Slide 3
Applications of hybrid perovskites
Optoelectronic applications:
Solar cells
LEDs
Solid State Lighting
Hybrid perovskite ABX3
A = Ammonium ion
B = Metal ion
X = Halide ion
Notes: 3
3

## Slide 4
Lead halide Perovskite
Low dimensional hybrid perovskite
Perovskite-type compounds are built from only corner sharing PbX6 octahedra
dPb-Pb ≈ 6 Å
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 4
4

## Slide 5
The discovery of functional hybrid perovskite
PbX2
+ HX acid
+ amine
Heating 20-100°C
Filtration
XRD
Synthesis
Optical Characterizations
Structural determination
Notes: 5
5

## Slide 6
The discovery of functional hybrid perovskite
PbX2
+ HX acid
+ amine
Heating 20-100°C
Filtration
XRD
Synthesis
Optical Characterizations
Structural determination
Notes: 6
6

## Slide 7
CCT
CRI
6924 K
6503 K
5705 K
4040 K
92
94
96
97
94
3156 K
Yuan, H. ; Qi, L.; Paris, M. ; Chen, F.; Shen, Q.; Faulques, E.; Massuyeau, F.; Gautier, R. Advanced Science (2021) 8(19), 2101407
A 70-fold reduction in the number of experiments relative to a grid-based search
Experimental validation
Optimization of a white phosphor
Machine learning guided discovery of phosphors
Notes: 7
7

## Slide 8
The discovery of functional hybrid perovskite
PbX2
+ HX acid
+ amine
Heating 20-100°C
Filtration
XRD
Synthesis
Optical Characterizations
Structural determination
Notes: 8
8

## Slide 9
1
2
Intensity (a.u.)
Intensity (a.u.)
2q (°)
Perovskite or not perovskite ?
X-ray diffraction patterns of new hybrid metal halides
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
3
4
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
Notes: 9
9
Dans l’ordre 24, 25, 26, 1

## Slide 10
CNN => Manière de traiter les DRX peut paraitre aberrante car on a jamais appris à faire comme cela
Accuracy of 92% at discriminating perovskites vs. non perovskites
998 crystal structures from the Cambridge Structural Database
Identification of the structure type for each structure: Perovskite / Non-perovskite
Simulation of the powder XRD patterns
80% for training 20% for validation
Dataset
A convolutional neural network
to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 10
10

## Slide 11
PROBLEM
SOLUTION
How to identify the important features for the neural network in the XRD patterns?
Hide some parts of the XRD patterns and calculate the accuracy
Intensity (a.u.)
2q (°)
A 8° to 10° (2q) / 9 to 11 Å
B 12.5° to 17.5° (2q) / 5 to 7 Å
C 17.5° to 29.5° (2q) / 3 to 5 Å
How the neural network
can identify perovskites?
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 11
11

## Slide 12
A 8° to 10° (2q) / 9 to 11 Å
B
12.5° to 17.5° (2q) / 5 to 7 Å
C
17.5° to 29.5° (2q) / 3 to 5 Å
Three identified features
Sums of XRD patterns
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
How the neural network
can identify perovskites?
Notes: 12
12

## Slide 13
A 8° to 10° (2q) / 9 to 11 Å
B
12.5° to 17.5° (2q) / 5 to 7 Å
C
17.5° to 29.5° (2q) / 3 to 5 Å
Three identified features
Sums of XRD patterns
What are these features ?
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
How the neural network
can identify perovskites?
Notes: 13
13

## Slide 14
A 8° to 10° (2q) / 9 to 11 Å
B
12.5° to 17.5° (2q) / 5 to 7 Å
C
17.5° to 29.5° (2q) / 3 to 5 Å
Three identified features
Sums of XRD patterns
What are these features ?
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
How the neural network
can identify perovskites?
Notes: 14
14

## Slide 15
A 8° to 10° (2q) / 9 to 11 Å
B
12.5° to 17.5° (2q) / 5 to 7 Å
C
17.5° to 29.5° (2q) / 3 to 5 Å
Three identified features
Sums of XRD patterns
What are these features ?
d ≈ 6 Å
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
How the neural network
can identify perovskites?
Notes: 15
15

## Slide 16
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 16
16
Dans l’ordre 24, 25, 26, 1

## Slide 17
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A = Non Perovskite
B = Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 17
17
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 18
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 18
18
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 19
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 19
19
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 20
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Non Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 20
20
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 21
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A
B
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Non Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 21
21
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 22
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A
B
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Non Perovskite
Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 22
22
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 23
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A
B
A
B
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Non Perovskite
Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 23
23
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 24
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A
B
A
B
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Non Perovskite
Perovskite
Perovskite
Our augmented ability to identify perovskites
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Notes: 24
24
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 25
1
2
3
4
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
Intensity (a.u.)
2q (°)
2q (°)
2q (°)
2q (°)
Perovskite or not perovskite ?
A
B
A
B
A
B
A
B
A = Non Perovskite
B = Perovskite
Non Perovskite
Non Perovskite
Perovskite
Perovskite
Massuyeau, F.; Broux, T.; Coulet, F.; Demessence, A.; Mesbah, A.; Gautier, R. Advanced Materials, (2022) 34(41)
Our augmented ability to identify perovskites
Notes: 25
25
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 26
The discovery of functional hybrid perovskite
PbX2
+ HX acid
+ amine
Heating 20-100°C
Filtration
XRD
Synthesis
Optical Characterizations
Structural determination
Notes: 26
26

## Slide 27
Laref, R.; Massuyeau, F.; Gautier, R. Small, (2023) Accepted
Can we predict before the synthesis?
Can we accurately predict the synthesis of hybrid perovskites before the synthesis?
Is the organic amine the determining factor ?
385 different organic amines involved in 626 different crystal structures
Dataset
Notes: 27
27
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 28
Laref, R.; Massuyeau, F.; Gautier, R. Small, (2023) Accepted
Can we predict before the synthesis?
Perovskite
Extracting organic cations as SMILES using CSD API
Prediction
627
CIFs collected from CSD
Organic molecules represented as SMILES
2756 descriptors and fingerprints for each structure
(input matrix X)
Structure type for each structure
(output y)
Non
Perovskite
Machine Learning algorithms
SMILES = Simplified Molecular Input Line Entry Specification
Notes: 28
28
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 29
Laref, R.; Massuyeau, F.; Gautier, R. Small, (2023) Accepted
Can we predict before the synthesis?
The number of –NH3+ can determine the structure type with an accuracy of 84.99%
The best algorithm (GBDT) with the best combination of 10 descriptors allows to reach an accuracy of 88.65 %
Notes: 29
29
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 30
Laref, R.; Massuyeau, F.; Gautier, R. Small, (2023) Accepted
Can we predict before the synthesis?
Why the presence of –NH3+ is so important to crystallize perovskite type structures?
Strong nucleophilic site between four [PbX6]2- corner-sharing octahedra of the perovskite structural type.
–NH3+ localizes in these sites and creates a dense hydrogen network with X- halide ions.
Notes: 30
30
Dans l’ordre 24, 25, 26, 1
8 à 10 pour non perov
12.5 à 17.5 pour perov

## Slide 31
Conclusion
Perovskite vs. Non Perovskite
from the use of molecular descriptors
Perovskite vs. Non Perovskite
from the powder XRD patterns
Identify the important features to better understand the mechanisms.
Notes: 31
31

## Slide 32
Acknowledgment
Fundings:
Collaborators:
Florian Massuyeau
Rachid Laref
THANK YOU FOR
YOUR ATTENTION